
                                                                                                                     
  [image: image3.jpg]- UNIVERSIDAD
‘ FACULTAD DE DE LAREPUBLICA
“ INGENIERIA URUGUAY





Title: Degradation Pathways and Regeneration Response in PEM Water Electrolyzer Assemblies: Combined Effects of Membrane Type and Catalyst Chemistry
G. Tejera1, R. Rojas 1, E. Teliz1,2, R. Faccio3, L. Fernández-Werner3, V. Diaz1*
1GIIE, IIQ, Facultad de Ingeniería, UdelaR, J. Herrera y Reissig 565, CP 11300, Montevideo, Uruguay.

2GIIE,Facultad de Ciencias, UdelaR, Iguá 4225, CP 11400, Montevideo, Uruguay

3Área Física, DETEMA, Facultad de Química, Isidoro de María 1614, CP 11800, Montevideo, Uruguay.

*verodiaz@fing.edu.uy
Proton exchange membrane water electrolysis (PEMWE) is one of the most promising technologies for green hydrogen production, although the long-term durability of membrane–electrode assemblies (MEAs) remains a major barrier to large-scale deployment. In this work, degradation behavior in PEMWE assemblies is comparatively discussed based on recent studies using Nafion™ N1110 and Nafion™ N115 membranes under controlled potentiostatic and galvanostatic operation at 60 °C (Tejera et al., 2024; Tejera et al., 2026). 

For the N1110-based MEA, assembled with Pt black at both electrodes, degradation during 168 h potentiostatic holds at 2.0 V was associated with a progressive decrease in current density, an increase in ohmic resistance, and longer electrochemical time constants, revealing deterioration in charge-transfer and transport processes. After regeneration in 1 M H₂SO₄, the MEA partially recovered its initial performance, and the degradation rate became approximately six times lower than before regeneration, suggesting that reversible contamination was a dominant contributor to the observed temporary performance losses (Tejera et al., 2024). 

For the N115-based MEA, which employed Pt black at the cathode and IrRuOx at the anode, potentiostatic operation at 2.0 V led to a current decay that stabilized near 204 μA h⁻¹ cm⁻², while galvanostatic operation required an additional ~50 mV over 168 h to sustain the target current, confirming progressive resistive degradation. Acid regeneration again produced partial recovery, but subsequent degradation accelerated to ~860 μA h⁻¹ cm⁻², indicating that regeneration could not prevent the accumulation of irreversible structural damage (Tejera et al., 2026). 

Overall, both studies demonstrate that PEMWE degradation results from a combination of reversible contamination and irreversible structural deterioration. While acid treatment can temporarily restore performance, the long-term response depends strongly on membrane–catalyst configuration and on the balance between interfacial, ohmic, and mass-transport degradation pathways (Tejera et al., 2024; Tejera et al., 2026).
References

Tejera, G., Rojas, R., Teliz, E., & Diaz, V. (2024). PEM electrolysis: Degradation study of N1110 assemblies for the production of green hydrogen. Electrochimica Acta, 500, 144716. 

Tejera, G., Teliz, E., Faccio, R., Fernandez-Werner, L., & Diaz, V. (2026). Degradation pathways in PEM water electrolyzers: Insights from Nafion™ N115 membranes with Pt black and Ir–Ru oxide catalysts. Fuel, 410, 137919. 

Biography

Verónica Díaz is a Chemical Engineer from Universidad de la República (1997), with a Master’s in Chemical Engineering (2003) and a PhD in Chemistry (2011). Since 2024, she has been Full Professor with full-time dedication at the Institute of Chemical Engineering, Faculty of Engineering, UdelaR. She is also a Grade 4 PEDECIBA researcher since 2020 and a Level II researcher in Uruguay’s National System of Researchers. She leads the Interdisciplinary Electrochemical Engineering Group. Her work addresses electrochemical engineering, green hydrogen production, storage and applications, and electric mobility. She has coauthored 56 international peer-reviewed journal articles, 72 conference presentations, and one book chapter.
Presenting author details 
Full name: Verónica Díaz Moreno
Contact number:+59899167684
Twitter account:
Linked In account: https://www.linkedin.com/in/ver%C3%B3nica-d%C3%ADaz-moreno-28b5a9191/
Session/ Theme name: Chemistry of Energy
Category: Oral presentation
Mode of presentation: Virtual
[image: image1.jpg]



[image: image2.png]|[®.

INSTITUTO DE
INGENIERIA QUIMICA





